Oil Treatment

TECHNICAL DATA/SL + PLUS(

| Description: | SL+PLUS( is a chlorine free oil treatment designed for engine treatment for Extended Protection and anti-wear enhancement. |
| --- | --- |
| Applications: | SL+PLUS( is an oil soluble treatment for extreme presoiled automotive and truck engine oils. |
| Advantages: | SL+PLUS( has no chlorine. Chlorinated compounds in the engine in contact with moisture and in the presence of trace soluble metals and high temperatures will create hydrochloric acid. As a result, serious corrosion problems develop. SL+PLUS( is free of solids. Use of solids (graphite, molybdenum disulfide or PTFE/Teflon ) suspended in oil is used to enhance lubricity but avoid corrosion problems of chlorine. The use of these chemicals can be inconsistent because the flow of solids is dependent solely upon mechanical means; protection is difficult to control since there is no uniform chemical reaction. SL+PLUS( contains no phosphorous which can contaminate the catalytic converter. SL+PLUS( prevents wear, has extreme pressure properties (EP) and reduces friction. These properties provide possible increased engine life, lower valve train wear and improved fuel economy. (see Tables 1, 2 and 3 on the reverse.) SL+PLUS( formulation follows the “Policy Guidelines for Use of Aftermarket Fuel and Lubricant Additives” issued May, 1996 by the Defense Department. The policy has two objectives: 1) the candidate product must deliver a measurable improvement and, 2) the presence of the candidate product must not cause any adverse side effects (corrosion, additive separation, etc.). |

Recent Tests SL + PLUS™

Table 1	SRV Machine Method A

| Blend | Coefficient of Friction | Wear | Appearance/Comments |
| --- | --- | --- | --- |
|  | Min/max | Plate/Cylinder |  |
| Engine Oil | 0.155µ/0.193µ | 1.42µm/0.28mm | Oil with flaky abrasive |
| 20% CET(1) | 0.168µ/0.194µ | 1.39µm/0.30mm | Some flaky abrasive |
| 10% SL+PLUS (2) | 0.112µ/0.163µ | 1.42µm/0.40mm | Almost non-abrasive |

Table 2	SRV Machine Method B

| Blend | Coefficient of Friction | Wear | Appearance/Comments |
| --- | --- | --- | --- |
|  | Min/max | Plate/Cylinder |  |
| Engine Oil | 0.150µ/0.157µ | 0.64µm/0.17mm | No abrasion |
| 20% CET(1) | 0.148µ/0.160µ | 0.58µm/0.25mm | No abrasion |
| 10% SL+ PLUS (2) | 0.113µ/0.124µ | 0.65µm/0.25mm | No abrasion |

Table 3	Falex & 4-Ball Wear

| Blend | Falex EP, lb | 4-Ball EP, kg |
| --- | --- | --- |
| Engine Oil | 1000 | 250 |
| 20% CET(1) | 750 | 200 |
| 10% SL+PLUS (2) | 3000 | 315 |

| Notes: |  |
| --- | --- |
| SRV Method A | (Steel/Aluminum) steel cylinder 100 CR 6 (AISI 52100), 15mm X 11mm ALSI plate; 50 Hz, load 50N, 100º C, amplitude 2mm, test duration 30 min. |
| SRV Method B | (Steel/Steel) steel cylinder 100 CR 6 (AISI 52100), 15mm X 11mm plate 100 CR 6 (AISI 52100); 50 Hz, load 50N, 100º C, amplitude 2mm, test duration 30 min. |
| Engine Oil | major brand 10W-30 API SJ engine oil |
| CET | Nationally available chlorinated-paraffin based engine treatment additive |
| (1) | percent by weight of CET in Engine Oil |
| (2) | percent by weight of SL PLUS+ in Engine Oil |